## Slide 1: Unexpected (sort of) Anisotropy of Cation & Anion Diffusion in Cr2O3
Penghui Cao1, Daniel Wells2, Dennis Hussey2, Michael Short1
1 Department of Nuclear Science and Engineering, MIT, USA
2 Electric Power Research Institute (EPRI), Palo Alto, CA & Charlotte, NC, USA
TMS-2016, Nashville, TN
February 15, 2016

## Slide 2: Multiscale Modeling of the CRUD Source Term
Chalk River Unidentified Deposits: Corrosion deposits on fuel rods
CRUD cross section showing typical structure
Corrosion products deposit as CRUD on fuel rods
CRUD constituent phases
Short, M. P.,et al. MRS-B 39(1):71-77 (2014)
To hot leg
To cold leg
CASL phase I scope
What about the CRUD source term?

## Slide 3: What Is CRUD? Why Does It Matter?
Chalk River Unidentified Deposits: Causes operational problems like:
Power
Core Height
Axial downward power shift
BO3 Concentration
CRUD induced power shift
“Leaker” fuel failures
CRUD-induced localized corrosion
Image: D. Wells. EPRI Summer P-TAC Meeting (2013)
Image: D. Gaston et al. Ann. Nucl. Ener., doi: 10.1016/j.anucene.2014.09.060 (2014)

## Slide 4: First: An Overall System View
Where does CRUD come/go in a PWR primary loop?
Cold Leg: 304SS, ~290C
Steam Generator: Alloy 600/690, 330C (Inlet) to 290C (Outlet)
Core: Contains fuel rods with sub-cooled boiling, removing particulates
Hot Leg: 304SS, ~330C

## Slide 5: Engineering Scale: What Is Missing?
Ultimate goal: Predict the Ni & Fe metal release terms
  Acts as source term for CRUD deposition codes (MAMBA1, BOA2)
1 Developed by CASL
2 Developed by EPRI
? ? ?

## Slide 6: Choosing What (NOT) To Model
NiFe2O4
(Ni,Fe)(Cr,Fe)2O4
(Ni,Fe)Cr2O4
Cr2O3
Metal with (Cr,Ni) depletion zone
Base alloy
Flow, Erosion
O
Fe
Cr
Diffusion/Transport
600 | 690 | 304
600 | 690 | 304
Low Ni,Fe High Ni,Fe
in coolant in coolant
[1] T. Devine, ibid
[2] S Cisse et al. Corr. Sci., 56:209-216 (2012).
[1] [1] [1] [1] [2]
Missing diffusivity data

## Slide 7: Computing Unknown Diffusivities

## Slide 8: Computing Unknown Diffusivities: Cr2O3
[1] R. Grimes. Phil. Mag. A, 72(3):651-668 (1995).
[2] Minervini et al., J. Mater. Chem., 10:2349-2354 (2000).
Buckingham potential: Compensates charge loss due to ionic defects [1-2]
Model: 18x18x6 hexagonal unit cell with periodic boundary conditions, 58,320 atoms

## Slide 9: Computing Unknown Diffusivities: O in Cr2O3
In-plane diffusion
Out-of-plane
Path 1
Path 2
Path 3
Path 4
Path 5
Path | Migration barrier (eV) | Jump distance (Å) | (in-plane) | (out of plane)
1 | 0.425 | 2.63 | 2.63 | 0
2 | 2.38 | 2.99 | 2.99 | 0
3 | 1.38 | 2.74 | 1.53 | 2.27
4 | 1.63 | 2.85 | 1.72 | 2.27
5 | 5.532 | 4.13 | 3.45 | 2.27
Path | Migration barrier (eV) | Jump distance (Å) |  | 
1 | 0.425 | 2.63 | 2.63 | 0
2 | 2.38 | 2.99 | 2.99 | 0
3 | 1.38 | 2.74 | 1.53 | 2.27
4 | 1.63 | 2.85 | 1.72 | 2.27
5 | 5.532 | 4.13 | 3.45 | 2.27

## Slide 10: Watching Oxygen Diffusion Mechanisms
Path | Migration barrier (eV) | Jump distance d (Å) | (in-plane) | (out of plane)
1 | 0.425 | 2.63 | 2.63 | 0
2 | 2.38 | 2.99 | 2.99 | 0
3 | 1.38 | 2.74 | 1.53 | 2.27
4 | 1.63 | 2.85 | 1.72 | 2.27
5 | 5.532 | 4.13 | 3.45 | 2.27
Path | Migration barrier (eV) | Jump distance d (Å) |  | 
1 | 0.425 | 2.63 | 2.63 | 0
2 | 2.38 | 2.99 | 2.99 | 0
3 | 1.38 | 2.74 | 1.53 | 2.27
4 | 1.63 | 2.85 | 1.72 | 2.27
5 | 5.532 | 4.13 | 3.45 | 2.27
What this means:
Oxygen diffuses mostly in-plane…
Atoms colored by displacement from original sites

## Slide 11: Watching Oxygen Diffusion Mechanisms
What this means:
Oxygen diffuses mostly in-plane… but out-of-plane jumps do happen.
Atoms colored by displacement from original sites
Path | Migration barrier (eV) | Jump distance d (Å) | (in-plane) | (out of plane)
1 | 0.425 | 2.63 | 2.63 | 0
2 | 2.38 | 2.99 | 2.99 | 0
3 | 1.38 | 2.74 | 1.53 | 2.27
4 | 1.63 | 2.85 | 1.72 | 2.27
5 | 5.532 | 4.13 | 3.45 | 2.27
Path | Migration barrier (eV) | Jump distance d (Å) |  | 
1 | 0.425 | 2.63 | 2.63 | 0
2 | 2.38 | 2.99 | 2.99 | 0
3 | 1.38 | 2.74 | 1.53 | 2.27
4 | 1.63 | 2.85 | 1.72 | 2.27
5 | 5.532 | 4.13 | 3.45 | 2.27

## Slide 12: Unknown Diffusivities: Cr in Cr2O3
1
2
3
4
5
Path | Migration barrier (eV) | Jump distance d (Å) | (in-plane) | (out-of-plane)
1 | 0.971 | 2.87 | 2.84 | 0.385
2 | 8.19 | 4.96 | 4.96 | 0
3 | 7.86 | 5.74 | 5.73 | 0.385
4 | 2.67 | 2.65 | 0 | 2.65
5 | 1.23 | 6.41 | 0 | 6.41
Path | Migration barrier (eV) | Jump distance d (Å) |  | 
1 | 0.971 | 2.87 | 2.84 | 0.385
2 | 8.19 | 4.96 | 4.96 | 0
3 | 7.86 | 5.74 | 5.73 | 0.385
4 | 2.67 | 2.65 | 0 | 2.65
5 | 1.23 | 6.41 | 0 | 6.41

## Slide 13: Watching Chromium Diffusion Mechanisms
1
2
3
4
5
What does this mean?
Cations migrate out-of-plane, which is very anisotropic.

## Slide 14: Full Cr2O3 Dataset for Oxygen
Mildly anisotropic (50%)

## Slide 15: Full Cr2O3 Dataset for Chromium
Highly anisotropic (30x)

## Slide 16: Effects of Dopant Cations
Ni slows oxygen diffusion more than Fe for both defects
At 1800K,
Diffusivity at 1800K | Interstitial diffusion () | Vacancy diffusion ()
 | 5.82∙10-11 | 2.29∙10-10
 | 2.67∙10-10 | 2.32∙10-10
Diffusivity at 1800K |  | 
 | 5.82∙10-11 | 2.29∙10-10
 | 2.67∙10-10 | 2.32∙10-10

## Slide 17: Diffusion Coefficients in Cr2O3
O diffusivity: x (plus doping effects)
Cr diffusivity: x
Fe diffusivity: x
Ni diffusivity: x

## Slide 18: Comparison to Recent Work
Same diffusivities studied by MD in Cr2O3, different results
J. Vaari. “Molecular dynamics simulations of vacancy diffusion in chromium(III) oxide, hematite, magnetite and chromite.” Solid State Ionics, 270:10-15 (2015).

## Slide 19: Check Calculations with Experimental Data
Check computed MD Cr2O3 data with tracer diffusion experiments
A. C. S. Sabioni et al. “Diffusion of iron in Cr2O3: polycrystals and thin films.” Mat. Sci. Eng. A, 392:254-261 (2005)
R. E. Lobing et al. “Diffusion of Cations in Chromia Layers Grown on Iron-Base Alloys.” Oxidation of Metals, 37(1-2) (1992)
Our Calcs:

## Slide 20: Comparison to Other Systems
Charged defect anisotropy is quite common in other systems
E. Kendricket al. Nat. Mater., 2007, 6, 871
Long-range, anisotropic diffusion by hand-to-hand tetrahedral in La1-xBa1+xGaO4x/2 by DFT
In-plane O diffusion by the vacancy mechanism, with oxygen ion density in red
A. Chroneos et al. J. Mater. Chem., 20:266-270 (2010)

## Slide 21: Implications of This Work
Differently oriented Cr2O3 will:
  Oxidize faster/slower
  Pass impurity cations more/less quickly
Different component processing methods may impart different Cr2O3 oxide textures, lead to varying performance
  Being observed in nuclear reactor steam generator tubes

## Slide 22: Implications of This Work
May not sound important… but…
  Reducing metal release in reactors by 2x could greatly alleviate corrosion deposit (CRUD) buildup on fuel rods
May guide processing treatments for steam generator tubes