## Slide 1: Multiscale Modeling of the CRUD Source Term in Pressurized Water Reactors
Penghui Cao1, Derek Gaston2, Daniel Wells3, Dennis Hussey3, Michael Short1
1 Department of Nuclear Science and Engineering, MIT, USA
Idaho National Laboratory, Idaho Falls, ID, USA
2 Electric Power Research Institute (EPRI), Palo Alto, CA & Charlotte, NC, USA
TMS-2016, Nashville, TN
February 15, 2016

## Slide 2: Multiscale Modeling for Nuclear Reactors
Many efforts, with CASL1 leading the way
1Consortium for the Advanced Simulation of Light Water Reactors
DENOVO 12x12
DENOVO 50x50
DeCART
Source: CASL 2012 Round Table Meeting

## Slide 3: Multiscale Modeling: Focus on CRUD
Chalk River Unidentified Deposits: Corrosion deposits on fuel rods
CRUD cross section showing typical structure
Corrosion products deposit as CRUD on fuel rods
CRUD constituent phases
Short, M. P.,et al. MRS-B 39(1):71-77 (2014)
To hot leg
To cold leg
CASL phase I scope
What about the CRUD source term?

## Slide 4: What Is CRUD? Why Does It Matter?
Chalk River Unidentified Deposits: Causes operational problems like:
Power
Core Height
Axial downward power shift
BO3 Concentration
CRUD induced power shift
“Leaker” fuel failures
CRUD-induced localized corrosion
Image: D. Wells. EPRI Summer P-TAC Meeting (2013)
Image: D. Gaston et al. Ann. Nucl. Ener., doi: 10.1016/j.anucene.2014.09.060 (2014)

## Slide 5: What Leads to CRUD?
There must be a source term, a sink, and a driving force
PWR Steam Generator
Sources: Wikimedia, Thermopedia

## Slide 6: Planning a Multiscale CRUD Model
Understand the system, and its basic physics
Choose the framework, craft a workflow
Make justified assumptions
Uncover missing parameters
Integrate
Validate
Validate again, then validate some more!

## Slide 7: First: An Overall System View
Where does CRUD come/go in a PWR primary loop?
Cold Leg: 304SS, ~290C
Steam Generator: Alloy 600/690, 330C (Inlet) to 290C (Outlet)
Core: Contains fuel rods with sub-cooled boiling, removing particulates
Hot Leg: 304SS, ~330C

## Slide 8: High-Level Model Overview
SG: Alloy 600 or 690
Releases Ni/Fe via corrosion through oxides
Absorbs Ni/Fe via NiFe2O4 growth
Core: Separate code
Absorbs Ni/Fe via crud growth
Model for now as a straight pipe w/temperature gradient
Hot/Cold Legs:
304 Stainless Steel
Releases Ni/Fe via corrosion through oxides
Absorbs Ni/Fe via NiFe2O4 growth
Model sections as straight or U-bend pipes
Impose temperature, compute oxidation at each point

## Slide 9: Next: Choose Main Approaches & Tools
Molecular Dynamics (LAMMPS, Sandia)
MOOSE Mesoscale Oxidation, Diffusion Path Analysis
E. Broitman, R. Becker et al. PRICM-8, 2013.
MOOSE MultiApps, Transfers
D. Gaston et al., INL Multiphysics Group, 2013.
Fill in missing parameters
Compute local metal release rates
Integrate entire system for total CRUD source term

## Slide 10: Planning for Flexibility, Expandability
Take the time to choose/develop your modeling framework
  We chose MOOSE, for its abstraction, expandability, and existing tools
  Finite element framework
  Contains many existing, useful modules for our CRUD source problem
Source: http://www.mooseframework.org/about/
Phase field module: Useful for oxidation kinetics
CRUD deposition
1D nodal fluid flow
HUGE existing fuel performance code

## Slide 11: Planning for Flexibility, Expandability
Take the time to develop an efficient workflow
  Learn scripting to automate tasks, regular expressions to script faster
  If you have to repeat yourself, stop and script!
Source: C. Doctorow. The Guardian, 12/4/2012

## Slide 12: Planning for Flexibility, Expandability
Think about the problem in a modular way
  Each piece of physics should be able to stand alone
  Decide on coupling strategy, interscale communication early
Will save lots of time later!
Multiphysics simulation framework for coupling CRUD and microstructure effects into fuel performance. Source: Gaston, D., et al. Ann. Nucl. Ener. 84:45-54 (2015).

## Slide 13: Planning for Flexibility, Expandability
Take the time to visualize intermediate variables
  Time spent now pays off 1,000x later
  Effectively sets up an automatic debugging system for you
Video: CRUD’s effects on the KAIST3A neutronics benchmark. Source: Computational Multiphysics Group, Idaho National Laboratory

## Slide 14: Delineating Scales and Interscale Communication
Molecular Dynamics (LAMMPS, Sandia)
MOOSE Mesoscale Oxidation, Diffusion Path Analysis
E. Broitman, R. Becker et al. PRICM-8, 2013.
MOOSE MultiApps, Transfers, RELAP-7
D. Gaston et al., INL Multiphysics Group, 2013.
Pre-computed diffusivity relations
Recalculate environmental conditions
Calculate local Fe, Ni release rates

## Slide 15: Engineering Scale: What Is Missing?
Ultimate goal: Predict the Ni & Fe metal release terms
  Acts as source term for CRUD deposition codes (MAMBA1, BOA2)
1 Developed by CASL
2 Developed by EPRI
? ? ?

## Slide 16: Microscale: What Is Missing?
Assumptions about which oxides are important
Diffusivity data to determine metal release fluxes

## Slide 17: Observations of CRUD from PWRs
Mostly NiFe2O4 crystallites
Some NiO, Fe3O4
Source term appears to be particulate
Short, M. P.,et al. MRS-B 39(1):71-77 (2014)

## Slide 18: Observations Become Justified Assumptions
Alloy 600 corrosion
Alloy 690 corrosion
Alloy 600 oxide film
P. Combrade et al. “OXIDATION OF NI BASE ALLOYS IN PWR WATER: OXIDE LAYERS AND ASSOCIATED DAMAGE TO THE BASE METAL.” Proceedings of the 12th International Conference on Environmental Degradation of Materials in Nuclear Power System – Water Reactors – Edited by T.R. Allen, P.J. King, and L. Nelson TMS (The Minerals, Metals & Materials Society), 2005
All reactor internals create NiFe2O4 outer oxide crystals

## Slide 19: Observations Become Justified Assumptions
Source: T. Devine. “Diffusion Path Analysis of Alloy 600’s and Alloy 690’s Passive Films and Understanding/Predicting Cation Release Rates.” P-TAC Presentation, Nov. 2013.
Saturation near 1ppb in PWR, fractions of a mole in 138m3 of coolant

## Slide 20: Choosing What (NOT) To Model
NiFe2O4
(Ni,Fe)(Cr,Fe)2O4
(Ni,Fe)Cr2O4
Cr2O3
Metal with (Cr,Ni) depletion zone
Base alloy
Flow, Erosion
O
Fe
Cr
Diffusion/Transport
600 | 690 | 304
600 | 690 | 304
Low Ni,Fe High Ni,Fe
in coolant in coolant
[1] T. Devine, ibid
[2] S Cisse et al. Corr. Sci., 56:209-216 (2012).
[1] [1] [1] [1] [2]
Missing diffusivity data

## Slide 21: Atomistic Scale: What Is Missing?
Diffusivity prefactors, activation energies for metal diffusion through oxides
  Mechanisms for diffusion of cations through oxides
Oxygen diffusion through Cr2O3
Cation diffusion through Cr2O3

## Slide 22: Computing Unknown Diffusivities

## Slide 23: Computing Unknown Diffusivities: Cr-Ni Metal
Cr
Ni10Cr90
Ni50Cr50
Build large cube of an Fe-Cr-Ni alloy, calculate system energy
Remove one atom at a time, recalculate system energy
Repeat steps 1-2 for every atom in every alloy, get statistics
Evf(Ni) is 1.39 eV
Evf(Cr) is 2.19 eV

## Slide 24: Computing Unknown Diffusivities: Alloy 600
Alloy 600 --Vacancy Formation and Migration Energies
Ni Vacancy
Cr Vacancy
Fe Vacancy

## Slide 25: Computing Unknown Diffusivities: Alloy 690
Alloy 690 --Vacancy Formation and Migration Energies

## Slide 26: Computing Unknown Diffusivities: Cr2O3
[1] R. Grimes. Phil. Mag. A, 72(3):651-668 (1995).
[2] Minervini et al., J. Mater. Chem., 10:2349-2354 (2000).
Buckingham potential: Compensates charge loss due to ionic defects [1-2]
Model: 18x18x6 hexagonal unit cell with periodic boundary conditions, 58,320 atoms

## Slide 27: Computing Unknown Diffusivities: O in Cr2O3
In-plane diffusion
Out-of-plane
Path 1
Path 2
Path 3
Path 4
Path 5
Path | Migration barrier (eV) | Jump distance (Å) | (in-plane) | (out of plane)
1 | 0.425 | 2.63 | 2.63 | 0
2 | 2.38 | 2.99 | 2.99 | 0
3 | 1.38 | 2.74 | 1.53 | 2.27
4 | 1.63 | 2.85 | 1.72 | 2.27
5 | 5.532 | 4.13 | 3.45 | 2.27
Path | Migration barrier (eV) | Jump distance (Å) |  | 
1 | 0.425 | 2.63 | 2.63 | 0
2 | 2.38 | 2.99 | 2.99 | 0
3 | 1.38 | 2.74 | 1.53 | 2.27
4 | 1.63 | 2.85 | 1.72 | 2.27
5 | 5.532 | 4.13 | 3.45 | 2.27

## Slide 28: Unknown Diffusivities: Cr in Cr2O3
1
2
3
4
5
Path | Migration barrier (eV) | Jump distance d (Å) | (in-plane) | (out-of-plane)
1 | 0.971 | 2.87 | 2.84 | 0.385
2 | 8.19 | 4.96 | 4.96 | 0
3 | 7.86 | 5.74 | 5.73 | 0.385
4 | 2.67 | 2.65 | 0 | 2.65
5 | 1.23 | 6.41 | 0 | 6.41
Path | Migration barrier (eV) | Jump distance d (Å) |  | 
1 | 0.971 | 2.87 | 2.84 | 0.385
2 | 8.19 | 4.96 | 4.96 | 0
3 | 7.86 | 5.74 | 5.73 | 0.385
4 | 2.67 | 2.65 | 0 | 2.65
5 | 1.23 | 6.41 | 0 | 6.41

## Slide 29: Diffusion Coefficients in Cr2O3
O diffusivity: x (plus doping effects)
Cr diffusivity: x
Fe diffusivity: x
Ni diffusivity: x

## Slide 30: Unknown Diffusivities: (Fe,Ni)Cr2O4
Compute with high vacancy density (like high temperature)
Scale down to correct temperature’s vacancy concentration

## Slide 31: Unknown Diffusivities: (Fe,Ni)Cr2O4
Compute with high vacancy density (like high temperature)
Scale down to correct temperature’s vacancy concentration

## Slide 32: Overall Diffusion Coefficients
O diffusivity: x
Cr diffusivity: x
Fe diffusivity: x
Ni diffusivity: x
Oxygen diffusivity: 1.9x + (1-r)*2.5x
Cr diffusivity: x + (1-r)*5.6x
Fe diffusivity: x
Ni diffusivity: x Composition: (FerNi(1-r))Cr2O4

## Slide 33: Microscale Model Assumptions
Source: T. Devine. “Diffusion Path Analysis of Alloy 600’s and Alloy 690’s Passive Films and Understanding/Predicting Cation Release Rates.” P-TAC Presentation, Nov. 2013.
304 Stainless Steel
Only the innermost oxide layer is protective
  NiFe2O4 growth happens from supersaturated coolant, not diffusive transport
    Just represents a time delay in particulate release of NiFe2O4, NiO

## Slide 34: Microscale Model Assumptions: Oxide Thickness
Used experimental data from oxidation of A600, A690, 304SS at PWR conditions
  325-350C, 1200ppm H3BO3, 2ppm LiOH, pH ~ 7.2, 25-30 cc/kg H2
Program on Technology Innovation: Review of Oxidation and Surface Film Formation Studies
on Austenitic Alloys in Light Water Reactor Coolants. EPRI, Palo Alto, CA: 2015. 3002005478
L. Guinard, C. Gabet, T. Czerwiec, E. Riquelme, and O. Kerrec, “Effect of surface passivation of Inconel 690 on oxidation in primary circuit conditions,” presented at the
Water Chemistry of Nuclear Reactor Systems 8, BNES, vol. 1, p. 67, 2000.
A. Machet, A. Galtayries, S. Zanna, P. Jolivet, M. Foucault, P. Combrade, P. Scott, and P. Marcus, “Kinetics of passivation of a nickel-base alloy in high temperature water,” presented at the EUROCORR 2004, Nice (France), 2004.

## Slide 35: Feed Microscale into Engineering Scale
Microscale model computes Fickian flux, feeds areal release rate up to engineering scale
A600, A690, SS304
Metal
Oxide
Prescribed thickness vs. time

## Slide 36: Feed Microscale into Engineering Scale
Assume grain boundary diffusivity increases lattice (bulk) diffusivities by ~3 orders of magnitude
A. C. S. Sabioni et al. “Diffusion of iron in Cr2O3: polycrystals and thin films.” Mat. Sci. Eng. A, 392:254-261 (2005)

## Slide 37: Putting it All Together
Compute local metal release rate at every location & time step
Diffusivities, oxide thicknesses are functions of space & time
  Temperature profiles prescribed along loop, also functions of space & time
Local release rate
Species i (Fe or Ni for now)
Quadrature point
Prescribed oxide thickness vs. time & type
Avogadro’s number
Atomic number density
Local wetted perimeter
Concentration of species i in local metal
Temperature-dependent diffusivity
Diffusion Flux (m2/s)

## Slide 38: Putting it All Together
Integrate to get total loop metal release vs. time
Uses MOOSE postprocessor to integrate
Account for deposition due to CRUD with any of:
Deposition factor
Erosion factor
Deposition rate
Loop particulate concentration
Boiling rate
Turbulent kinetic energy from CFD
Wetted perimeter

## Slide 39: The (First) Final Result
Remember our goal: Predict Ni, Fe release rates

## Slide 40: Intermediate Variables: Geometry, Diffusivity
Steam Generator
Cold Leg
Hot Leg
Core

## Slide 41: Intermediate Variables: Oxide Thickness
Steam Generator
Cold Leg
Hot Leg
Core

## Slide 42: Intermediate Variables: Release Rates (Linear)
Steam Generator
Cold Leg
Hot Leg
Core

## Slide 43: Intermediate Variables: Release Rates (Log)
Steam Generator
Cold Leg
Hot Leg
Core

## Slide 44: Validation: Single-Effect
Check computed MD Cr2O3 data with tracer diffusion experiments
A. C. S. Sabioni et al. “Diffusion of iron in Cr2O3: polycrystals and thin films.” Mat. Sci. Eng. A, 392:254-261 (2005)
R. E. Lobing et al. “Diffusion of Cations in Chromia Layers Grown on Iron-Base Alloys.” Oxidation of Metals, 37(1-2) (1992)
Our Calcs:

## Slide 45: Validation: Single-Effect
Check computed MD Cr2O3 data with tracer diffusion experiments
M. G. E. Cox, B. McEnaney, and V. D. Scott, Phil. Mag. 26, 839 (1972).
Our Calculations:

## Slide 46: Microscale Validation
Can the impurity cation concentration be so large in Cr2O3?
Yes!
A.C.S. Sabioni et al. Solid State Ionics, 276:188 (2015)

## Slide 47: PWR Plant (Integrated) Validation
Observation 1: CRUD is mostly Ni-oxides
  We predict Ni-release outpacing Fe-release after one year
Observation 2: About 10,000 moles of metal released
  CRUD loading in PWR fuel is around 10’s of kg

## Slide 48: What Comes Next?
Targeted questions for industry
  Is there an Fe-release upon steam generator replacement?
  What is the distribution of CRUD loading over time?
Additional validation needs: experiments
  Targeted analysis of steam generator tubes post-failure
  Measure CRUD composition vs. thickness (like an archeological record)
Swap in new, more physical modules!

## Slide 49: Tip: Choose Your Framework Wisely
Nano/Micro simulation time: ~1 year
Engineering scale coding time: ~45 hours
  … plus a lot of planning
Source: http://www.mooseframework.org/about/

## Slide 50: Tip: Spend the Time to Write Modular Code
MD Diffusivity Data
Prescribed Oxides & Thicknesses from Literature Data
1D Diffusivity Model for Metal Release
Simple ODEs for Metal Release
Density Functional Theory (DFT) Diffusivity Data
Oxide thicknesses computed by MOOSE phase field module
RELAP-7 coolant temperatures
Prescribed temperatures
2D or 3D diffusivity model with grain boundaries
BISON fuel performance
MAMBA CRUD growth
Opportunities to combine multiscale with multiphysics

## Slide 51: Tip: Visualize Intermediate Variables
Great help in debugging more and more complex models

## Slide 52: Parting Notes: Take Control of Validation!
Actual Autoclave
Final Autoclave Drawing
Sapphire
Windows
Water out
Water in
Sample rod

## Slide 53: Parting Notes: Take Control of Validation!
Pressure switch
Fill Terminal
Pressurizing Pump
Pre-heater
From Water Tank
Vacuum Terminal
To Vent
    Differential Pressure Sensor
Circulation Pump
Control Valve
Control Valve
Thermocouple
1 Inch tubing
3/4 Inch tubing
1/2 Inch tubing
1/4 Inch tubing
To Measurement Loop
Autoclave